## Slide 1
Introduction
Deep Learning for Automated Defect Detection in TEM Images: RetinaNet
Dongxia Wu1, Varun Sreenivasan1, Vanessa Nilsen1, Mingren Shen1, and Dane Morgan1
1University of Wisconsin-Madison
Methods and Major Activities
Lin, et al. “Focal Loss for Dense Object Detection.” [1402.1128] Long Short-Term Memory Based Recurrent Neural Network Architectures for Large Vocabulary Speech Recognition, 7 Feb. 2018, arxiv.org/abs/1708.02002.
Fizyr. “Fizyr/Keras-Retinanet.” GitHub, 18 July 2018, github.com/fizyr/keras-retinanet.
Li, Wei, Kevin G. Field, and Dane Morgan. "Automated defect analysis in electron microscopic images." npj Computational Materials 4.1 (2018): 36
References
Results
Conclusions
The model still has further scope for improvement, especially recall. The following methods can be used:
Preparing a larger dataset comprising of more micrographs of irradiated metals, focusing on smaller defects.
Train the model for a longer duration.
Future Work
The model performs reasonably well in terms of recall and precision. However, there is still room for improvement:
The model has an average recall of 68% and average precision of 85% on the test set.
Relatively low recall stems from inability to detect small defects.
Data Preparation
A dataset of 298 micrograph images with 9566 total loop defects (3) was prepared by two researchers experienced in loop-labelling (set as “ground truth”)
The dataset was split into a training set and testing set at a fixed 9:1 ratio. After splitting, a training set of 270 images and test set of 20 images were obtained (3).
Training Model
Multiple RetinaNet models were created by varying hyperparameters such as number of epochs, number of layers, batch size, and learning rate.
Optimal parameters values were obtained by testing the various models.
Testing Model
Recall and Precision metrics were used to quantify the performance of the model.
The best model was selected by determining the model that maximizes recall and precision values and minimizes the difference between the two values.
“RetinaNet is a single, unified network composed of a backbone and two task-specific subnetworks”. The FPN backbone on top of feedforward ResNet architecture helps generate a rich, multiscale convolutional feature pyramid (2). The model also utilizes the focal loss function that helps mitigate the accuracy gap between one and two stage detectors (2).
Fig 2: RetinaNet architecture (2)
Model Summary
Ground Truth
Predicted Labels
Recall: 74% Precision: 89% F1 Score: 0.81
Fig 3: Recall vs Size of Loops
Fig 4: Precision vs Size of Loops
Fig 5: Ground Truth Labels vs Predicted Labels
Fig 3’s 0-500 pixels2 group suggests the model doesn’t work well for small defects.
Recall improves sharply in the 0-1000 pixels2 region because the model is able to better discern defects.
Fig 4 suggests that there is no coherent relationship between loop size and precision.
Precision seems to be affected by the model’s inability to effectively differentiate between 111, 100, and pre-existing defects
RECALL AND PRECISION TRENDS
Classifying defects in metallic microstructures is done widely in the metallographic industry to understand and assess the quality and performance of metal alloys. In nuclear applications this process is critical to understand the effects of radiation and design for safe operation of nuclear reactors.
Ground Truth Labeling
Currently defects are frequently identified through electron microscopy, and the image analysis is done by hand, which is slow, error prone and inconsistent.
Our project focused on automating this process using computer vision techniques based on convolution neural networks. The Univ. of WI team is exploring four implementations of networks, and this project is focused on one known as RetinaNet [1].
1
2
3
4
5
6
7
8
9
10
11
12
11
ResNet
Feature pyramid net
Funding by Schmidt Futures grant number MSN214683 as part of Citrine Informatics’ NextGen Fellowship
Funding & Acknowledgements
Notes: Consider making an appointment with https://designlab.wisc.edu/make-an-appointment to review your poster.